APPROVAL SHEET

MODEL NO.：

CUSTOMER：

CUSTOMER'S APPROVAL： AUTHORIZED SIGNATURE/STAMP DATE

MANUFACTURER: LaoHuLing Industrial Area, XiaoJinKou Town, HuiCheng District, HuiZhou City, GuangDong Province, CHINA Tel: 0752-7213069/7213070 Fax: 0752-7213065 Submitted by: Approved by: Date:

Performance Specification

| Model | Marking |  |  |  |  |  | Maximum | Resistance | 认证 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | V max | Imax | I hold | I trip | Pd | Time To Trip |  |  |
|  |  |  |  | @25°C | @25°C | Typ. | Current | Time | R i min | R1max | UL |
|  |  | (V dc) | (A) | (A) | (A) | (W) | (A) | (Sec) | () | () |  |
| SMD1210R005SF | RA | 30.0 | 30 | 0.05 | 0.15 | 0.6 | 0.25 | 1.50 | 2.800 | 50.000 |  |
| SMD1210R005SF13.2V | RA | 13.2 | 30 | 0.05 | 0.15 | 0.6 | 0.25 | 1.50 | 2.800 | 50.000 | √ |
| SMD1210R010SF | R1 | 30.0 | 30 | 0.10 | 0.30 | 0.6 | 0.50 | 0.60 | 0.800 | 15.000 |  |
| SMD1210R010SF13.2V | R1 | 13.2 | 30 | 0.10 | 0.30 | 0.6 | 0.50 | 0.60 | 1.600 | 15.000 | √ |
| SMD1210R020SF | R2 | 30.0 | 30 | 0.20 | 0.40 | 0.6 | 8.0 | 0.02 | 0.400 | 5.000 |  |
| SMD1210R020SF13.2V | R2 | 13.2 | 30 | 0.20 | 0.40 | 0.6 | 8.0 | 0.02 | 0.400 | 5.000 | √ |
| SMD1210R035SF | R3 | 6.0 | 30 | 0.35 | 0.75 | 0.6 | 8.0 | 0.20 | 0.200 | 1.300 | √ |
| SMD1210R035SF | R3 | 13.2 | 30 | 0.35 | 0.75 | 0.6 | 8.0 | 0.20 | 0.200 | 1.300 | √ |
| SMD1210R035SF16v | R3 | 16.0 | 30 | 0.35 | 0.75 | 0.6 | 8.0 | 0.20 | 0.200 | 1.300 |  |
| SMD1210R050SF | R5 | 13.2 | 30 | 0.50 | 1.00 | 0.6 | 8.0 | 0.10 | 0.180 | 0.900 | √ |
| SMD1210R050SF24v | R5 | 24.0 | 30 | 0.50 | 1.00 | 0.6 | 8.0 | 0.10 | 0.180 | 0.900 |  |
| SMD1210R075SF | R7 | 6.0 | 30 | 0.75 | 1.50 | 0.6 | 8.0 | 0.10 | 0.070 | 0.400 | √ |
| SMD1210R075SF16v | R7 | 16.0 | 30 | 0.75 | 1.50 | 0.6 | 8.0 | 0.10 | 0.070 | 0.400 |  |
| SMD1210R110SF | R0 | 6.0 | 35 | 1.10 | 2.20 | 0.6 | 8.0 | 0.30 | 0.050 | 0.210 | √ |
| SMD1210R150SF | RX | 6.0 | 35 | 1.50 | 3.00 | 0.6 | 8.0 | 0.50 | 0.030 | 0.110 | √ |
| SMD1210R150SF12v | RX | 12.0 | 35 | 1.50 | 3.00 | 0.6 | 8.0 | 0.50 | 0.030 | 0.110 |  |
| SMD1210R175SF | RY | 6.0 | 35 | 1.75 | 3.50 | 0.8 | 8.0 | 0.60 | 0.020 | 0.080 | √ |
| SMD1210R200SF | RZ | 6.0 | 35 | 2.00 | 4.00 | 0.8 | 8.0 | 1.00 | 0.015 | 0.070 | √ |
| SMD1210R260SF | R— | 6.0 | 35 | 2.60 | 5.20 | 0.8 | 8.0 | 2.00 | 0.010 | 0.060 |  |

V max  = Maximum operating voltage device can withstand without damage at rated current (Imax).

I max   = Maximum fault current device can withstand without damage at rated voltage (V max).

I hold   = Hold Current. Maximum current device will not trip in 25°C still air.

I trip    = Trip Current. Minimum current at which the device will always trip in 25°C still air.

Pd      = Power dissipation when device is in the tripped state in 25°C still air environment at rated voltage.

Ri min/max  = Minimum/Maximum device resistance prior to tripping at 25°C.

R1max  = Maximum device resistance is measured one hour post reflow.

CAUTION : Operation beyond the specified ratings may result in damage and possible arcing and flame.

Environmental Specifications

| Test |  |  |  | Conditions |  |  |  | Resistance change |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Passive aging |  |  |  | +85°C, 1000 hrs. |  |  | ±5% typical |  |  |
| Humidity aging |  |  |  | +85°C, 85% R.H. , 168 hours |  | ±5% typical |  |  |
| Thermal shock |  |  |  | +85°C to -40°C, 20 times |  |  | ±33% typical |  |
| Resistance to solvent |  |  |  | MIL-STD-202,Method 215 |  |  | No change |  |  |
| Vibration |  |  |  | MIL-STD-202,Method 201 |  |  | No change |  |  |
| Ambient operating conditions : - 40 °C to +85 °C |  |  |
| Maximum surface temperature of the device in the tripped state is 125 °C |

Agency Approval and Environmental Complianc

| Agency | File Number |  | Regulation | Standard |
| --- | --- | --- | --- | --- |
| UL | E486890 |  |  | 2002/95/EC |
| TUV | pending |  |  | EN14582 |

Thermal Derading Chart

Recommended Hold Current(A) at Ambient Temperature(°C)

| Model | Ambient Operation Temperature |
| --- | --- |
|  | -40°C | -20°C | 0°C | 25°C | 40°C | 50°C | 60°C | 70°C | 85°C |
| SMD1210R005SF | 0.08 | 0.07 | 0.06 | 0.05 | 0.04 | 0.04 | 0.03 | 0.03 | 0.02 |
| SMD1210R010SF | 0.16 | 0.14 | 0.12 | 0.10 | 0.08 | 0.07 | 0.06 | 0.05 | 0.03 |
| SMD1210R020SF | 0.29 | 0.26 | 0.22 | 0.20 | 0.16 | 0.14 | 0.13 | 0.11 | 0.08 |
| SMD1210R035SF | 0.47 | 0.45 | 0.40 | 0.35 | 0.33 | 0.28 | 0.24 | 0.21 | 0.18 |
| SMD1210R050SF | 0.76 | 0.67 | 0.58 | 0.50 | 0.43 | 0.40 | 0.36 | 0.32 | 0.28 |
| SMD1210R075SF | 1.00 | 0.97 | 0.86 | 0.75 | 0.64 | 0.59 | 0.54 | 0.48 | 0.40 |
| SMD1210R110SF | 1.69 | 1.48 | 1.29 | 1.10 | 0.88 | 0.76 | 0.65 | 0.57 | 0.43 |
| SMD1210R150SF | 2.13 | 1.92 | 1.71 | 1.50 | 1.26 | 1.14 | 1.01 | 0.89 | 0.71 |
| SMD1210R175SF | 2.54 | 2.30 | 2.02 | 1.75 | 1.47 | 1.33 | 1.18 | 1.05 | 0.86 |
| SMD1210R200SF | 2.90 | 2.63 | 2.31 | 2.00 | 1.68 | 1.52 | 1.35 | 1.20 | 0.98 |
| SMD1210R260SF | 3.43 | 3.22 | 2.93 | 2.60 | 2.23 | 2.03 | 1.87 | 1.57 | 1.35 |

Thermal Derating Curve                  Average Time-Current Curve

Soldering Parameters

| Profile Feature | Pb-Free Assembly |
| --- | --- |
| Average Ramp-Up Rate(Ts max to T p) | 3℃/second mac. |
| Preheat -Temperature Min(Ts min) -Temperature Max(Ts max) -Time(Ts min to Ts max) | 150℃ 200℃ 60~180 seconds |
| Time maintained above: -Temperature(TL) -Time(tL) | 217℃ 60~150 seconds |
| Peak Temperature(Tp) | 260℃ |
| Ramp-Down Rate | 6℃/second max. |
| Time 25℃ to Peak Temperature | 8 minutes max |
| Storage Condition | 0℃~35℃,30%~60%RH |

Recommended reflow methods: IR, vapor phase oven, hot air oven, N2 environment for lead-free

Recommended maximum paste thickness is 0.25mm

Devices can be cleaned using standard industry methods and solvents.

Note 1:All temperature refer to topside of the package, measured on the package body surface.

Note 2: If reflow temperatures exceed the recommended profile, devices may not meet the performance requirements.

Physical Dimensions(mm.)

| Model | A | B | C | D | E |
| --- | --- | --- | --- | --- | --- |
|  | Min. | Max. | Min. | Max. | Min. | Max. | Min. | Min. |
| SMD1210R005SF | 3.00 | 3.50 | 2.35 | 2.80 | 0.60 | 1.20 | 0.30 | 0.10 |
| SMD1210R005SF13.2V | 3.00 | 3.50 | 2.35 | 2.80 | 0.60 | 1.20 | 0.30 | 0.10 |
| SMD1210R010SF | 3.00 | 3.50 | 2.35 | 2.80 | 0.60 | 1.20 | 0.30 | 0.10 |
| SMD1210R010SF13.2V | 3.00 | 3.50 | 2.35 | 2.80 | 0.60 | 1.20 | 0.30 | 0.10 |
| SMD1210R020SF | 3.00 | 3.50 | 2.35 | 2.80 | 0.50 | 1.10 | 0.30 | 0.10 |
| SMD1210R020SF13.2V | 3.00 | 3.50 | 2.35 | 2.80 | 0.50 | 1.10 | 0.30 | 0.10 |
| SMD1210R035SF | 3.00 | 3.50 | 2.35 | 2.80 | 0.50 | 1.10 | 0.30 | 0.10 |
| SMD1210R035SF13.2V | 3.00 | 3.50 | 2.35 | 2.80 | 0.50 | 1.10 | 0.30 | 0.10 |
| SMD1210R035SF16V | 3.00 | 3.50 | 2.35 | 2.80 | 0.50 | 1.10 | 0.30 | 0.10 |
| SMD1210R050SF | 3.00 | 3.50 | 2.35 | 2.80 | 0.50 | 1.10 | 0.30 | 0.10 |
| SMD1210R050SF24V | 3.00 | 3.50 | 2.35 | 2.80 | 0.50 | 1.10 | 0.30 | 0.10 |
| SMD1210R075SF | 3.00 | 3.50 | 2.35 | 2.80 | 0.50 | 1.10 | 0.30 | 0.10 |
| SMD1210R075SF16V | 3.00 | 3.50 | 2.35 | 2.80 | 0.50 | 1.10 | 0.30 | 0.10 |
| SMD1210R110SF | 3.00 | 3.50 | 2.35 | 2.8 | 0.50 | 1.10 | 0.30 | 0.10 |
| SMD1210R150SF | 3.00 | 3.50 | 2.35 | 2.80 | 0.50 | 1.20 | 0.30 | 0.10 |
| SMD1210R150SF12V | 3.00 | 3.50 | 2.35 | 2.80 | 0.50 | 1.20 | 0.30 | 0.10 |
| SMD1210R175SF | 3.00 | 3.50 | 2.35 | 2.80 | 0.80 | 1.40 | 0.30 | 0.10 |
| SMD1210R200SF | 3.00 | 3.50 | 2.35 | 2.80 | 0.80 | 1.40 | 0.30 | 0.10 |
| SMD1210R260SF | 3.00 | 3.50 | 2.35 | 2.80 | 1.00 | 1.60 | 0.30 | 0.10 |

Termination Pad Characteristics

Terminal pad materials：Tin-plated Nickel-Copper

Terminal pad solder ability：Meets EIA specification RS186-9E and ANSI/J-STD-002 Category 3.

Recommended Pad Layout (mm.)

Packaging Quantity

| Part Number | Quantity |
| --- | --- |
| SMD1210 | 4000 pcs/reel |

Tape & reel packaging per EIA481-1

Tape And Reel Specifications (mm)

| Governing Specifications | EIA 481-1 |
| --- | --- |
| W |  | 8.15 ± 0.2 |
| P0 |  | 4.0 ± 0.10 |
| P1 |  | 4.0 ± 0.10 |
| P2 |  | 2.0 ± 0.05 |
| A0 |  | 2.82 ± 0.10 |
| B0 |  | 3.52 ± 0.10 |
| B1max. |  | 4.35 |
| D0 |  | 1.50 + 0.1, -0 |
| F |  | 3.5 ± 0.05 |
| E1 |  | 1.75 ± 0.10 |
| E2min. |  | 6.25 |
| T |  | 0.6 |
| T1max. |  | 0.1 |
| K0 |  | 1.04 ± 0.1 |
| Leader min. |  | 390 |
| Trailer min. |  | 160 |
| Reel Dimensions |  |
| A max. |  | 178 |
| N min. |  | 60 |
| W1 |  | 9 ± 0.5 |
| W2 |  | 12.6 ± 0.5 |
| Storage And Handling |
| ‧ Storage conditions：35°C max,30%~60% R.H. |
| ‧ Devices may not meet specified performance |
| if storage conditions are exceeded. |

Part Number System

SMD 1210 R 口口口 S F  口口V
                                           special voltage Rating(Optional)

Lead-Free

Tin-plated Nickel-Copper

Holding Current Rating

Da Rong

Device Dimensions: Length/width(Unit:1/100 inch) Size 3225 mm / 1210 inch

Surface Mount Device

# Text boxes

t L

60~150 s

ts

Preheat 60~180 s

t 25°C to peak

Time

TL 217

TP 260

25

TP 20~40 S

Ramp-up

Critical Zone

TL to TP

Ramp-down

Tsmax

Tsmin

150

200

C

E

B

A

D

2

2.0士0.1

1.0士0.1

1.0 士0.1

2.5士0.1

P1

W

E2

F

E1

P0

P2

B0

K0

B1

T1

Cover tape

D0

A0

Embossment

T

EIA Tape Component Dimensions

Embossed cavity

Cover tape

Carrier tape

A

W2(measured at hub)

N(hub dia.)

W1(measured at hub)

2

2

2

0

EIA Reel Dimensions