APPROVAL SHEET

MODEL NO.：

CUSTOMER：

CUSTOMER'S APPROVAL： AUTHORIZED SIGNATURE/STAMP DATE

MANUFACTURER: LaoHuLing Industrial Area, XiaoJinKou Town, HuiCheng District, HuiZhou City, GuangDong Province, CHINA Tel: 0752-7213069/7213070 Fax: 0752-7213065 Submitted by: Approved by: Date:

Performance Specification

| Model | Marking |  |  |  |  |  | Maximum | Resistance | 认证 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | V max | Imax | I hold | I trip | Pd | Time To Trip |  |  |
|  |  |  |  | @25°C | @25°C | Typ. | Current | Time | R i min | R1max | UL |
|  |  | (Vdc) | (A) | (A) | (A) | (W) | (A) | (Sec) | () | () |  |
| SMD0805R005SF | 1 | 15.0 | 30 | 0.05 | 0.15 | 0.5 | 0.5 | 1.50 | 1.500 | 18.000 | √ |
| SMD0805R010SF | 1 | 15.0 | 30 | 0.10 | 0.30 | 0.5 | 0.5 | 1.50 | 0.750 | 6.000 | √ |
| SMD0805R020SF | 2 | 9.0 | 30 | 0.20 | 0.50 | 0.5 | 8.0 | 0.02 | 0.550 | 3.500 | √ |
| SMD0805R035SF | 3 | 6.0 | 30 | 0.35 | 0.75 | 0.5 | 8.0 | 0.10 | 0.200 | 1.200 | √ |
| SMD0805R035SF12v | 3 | 12.0 | 30 | 0.35 | 0.75 | 0.5 | 8.0 | 0.10 | 0.200 | 1.200 |  |
| SMD0805R050SF | 5 | 6.0 | 30 | 0.50 | 1.00 | 0.5 | 8.0 | 0.10 | 0.100 | 0.850 | √ |
| SMD0805R050SF12v | 5 | 12.0 | 30 | 0.50 | 1.00 | 0.5 | 8.0 | 0.10 | 0.100 | 0.850 |  |
| SMD0805R050SF16v | 5 | 16.0 | 30 | 0.50 | 1.00 | 0.5 | 8.0 | 0.10 | 0.100 | 0.850 |  |
| SMD0805R050SF24v | 5 | 24.0 | 30 | 0.50 | 1.00 | 0.5 | 8.0 | 0.10 | 0.100 | 0.850 |  |
| SMD0805R075SF | 7 | 6.0 | 35 | 0.75 | 1.50 | 0.6 | 8.0 | 0.20 | 0.070 | 0.385 | √ |
| SMD0805R075SF12v | 7 | 12.0 | 35 | 0.75 | 1.50 | 0.6 | 8.0 | 0.20 | 0.070 | 0.385 |  |
| SMD0805R100SF | 0 | 6.0 | 35 | 1.00 | 1.95 | 0.6 | 8.0 | 0.30 | 0.040 | 0.230 | √ |
| SMD0805R100SF12v | 0 | 12.0 | 35 | 1.00 | 1.95 | 0.6 | 8.0 | 0.30 | 0.040 | 0.230 |  |
| SMD0805R110SF | 0 | 6.0 | 35 | 1.10 | 2.20 | 0.6 | 8.0 | 0.30 | 0.035 | 0.210 | √ |
| SMD0805R110SF12v | 0 | 12.0 | 35 | 1.10 | 2.20 | 0.6 | 8.0 | 0.30 | 0.035 | 0.210 |  |
| SMD0805R125SF | 12 | 6.0 | 35 | 1.25 | 2.50 | 1.5 | 8.0 | 0.60 | 0.025 | 0.140 | √ |
| SMD0805R150SF | 15 | 6.0 | 35 | 1.50 | 3.00 | 1.0 | 8.0 | 0.50 | 0.015 | 0.130 | √ |

V max  = Maximum operating voltage device can withstand without damage at rated current (Imax).

I max   = Maximum fault current device can withstand without damage at rated voltage (V max).

I hold   = Hold Current. Maximum current device will not trip in 25°C still air.

I trip    = Trip Current. Minimum current at which the device will always trip in 25°C still air.

Pd      = Power dissipation when device is in the tripped state in 25°C still air environment at rated voltage.

Ri min/max  = Minimum/Maximum device resistance prior to tripping at 25°C.

R1max  = Maximum device resistance is measured one hour post reflow.

CAUTION : Operation beyond the specified ratings may result in damage and possible arcing and flame.

Environmental Specifications

| Test |  |  |  | Conditions |  |  |  | Resistance change |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Passive aging |  |  |  | +85°C, 1000 hrs. |  |  | ±5% typical |  |  |
| Humidity aging |  |  |  | +85°C, 85% R.H. , 168 hours |  | ±5% typical |  |  |
| Thermal shock |  |  |  | +85°C to -40°C, 20 times |  |  | ±33% typical |  |
| Resistance to solvent |  |  |  | MIL-STD-202,Method 215 |  |  | No change |  |  |
| Vibration |  |  |  | MIL-STD-202,Method 201 |  |  | No change |  |  |
| Ambient operating conditions : - 40 °C to +85 °C |
| Maximum surface temperature of the device in the tripped state is 125 °C |

Agency Approval and Environmental Complianc

| Agency | File Number |  | Regulation | Standard |
| --- | --- | --- | --- | --- |
| UL | E486890 |  |  | 2011/65/EU |
| TUV | pending |  |  | EN14582 |

Thermal Derading Chart

Recommended Hold Current(A) at Ambient Temperature(°C)

| Model | Ambient Operation Temperature |
| --- | --- |
|  | -40°C | -20°C | 0°C | 25°C | 40°C | 50°C | 60°C | 70°C | 85°C |
| SMD0805R005SF | 0.070 | 0.060 | 0.055 | 0.050 | 0.040 | 0.035 | 0.030 | 0.025 | 0.015 |
| SMD0805R010SF | 0.14 | 0.12 | 0.11 | 0.10 | 0.08 | 0.07 | 0.06 | 0.05 | 0.03 |
| SMD0805R020SF | 0.28 | 0.25 | 0.23 | 0.20 | 0.17 | 0.14 | 0.12 | 0.10 | 0.07 |
| SMD0805R035SF | 0.47 | 0.44 | 0.39 | 0.35 | 0.30 | 0.27 | 0.24 | 0.20 | 0.14 |
| SMD0805R050SF | 0.68 | 0.62 | 0.55 | 0.50 | 0.40 | 0.37 | 0.33 | 0.29 | 0.23 |
| SMD0805R075SF | 1.00 | 0.90 | 0.79 | 0.75 | 0.63 | 0.57 | 0.53 | 0.41 | 0.34 |
| SMD0805R100SF | 1.35 | 1.25 | 1.15 | 1.00 | 0.82 | 0.74 | 0.65 | 0.55 | 0.42 |
| SMD0805R110SF | 1.45 | 1.35 | 1.20 | 1.10 | 0.92 | 0.84 | 0.75 | 0.65 | 0.52 |
| SMD0805R125SF | 1.65 | 1.53 | 1.36 | 1.25 | 1.05 | 0.95 | 0.85 | 0.74 | 0.59 |
| SMD0805R150SF | 1.98 | 1.84 | 1.63 | 1.50 | 1.26 | 1.14 | 1.02 | 0.88 | 0.71 |

Thermal Derating Curve                Average Time-Current Curve

Soldering Parameters

| Profile Feature | Pb-Free Assembly |
| --- | --- |
| Average Ramp-Up Rate(Ts max to T p) | 3℃/second mac. |
| Preheat -Temperature Min(Ts min) -Temperature Max(Ts max) -Time(Ts min to Ts max) | 150℃ 200℃ 60~180 seconds |
| Time maintained above: -Temperature(TL) -Time(tL) | 217℃ 60~150 seconds |
| Peak Temperature(Tp) | 260℃ |
| Ramp-Down Rate | 6℃/second max. |
| Time 25℃ to Peak Temperature | 8 minutes max |
| Storage Condition | 0℃~35℃,30%-60%RH |

Recommended reflow methods: IR, vapor phase oven, hot air oven, N2 environment for lead-free

Recommended maximum paste thickness is 0.25mm

Devices can be cleaned using standard industry methods and solvents.

Note 1:All temperature refer to topside of the package, measured on the package body surface.

Note 2: If reflow temperatures exceed the recommended profile, devices may not meet the performance requirements.

Physical Dimensions(mm.)

| 型號 | A | B | C | D | E |
| --- | --- | --- | --- | --- | --- |
|  | Min. | Max. | Min. | Max. | Min. | Max. | Min. | Min. |
| SMD0805R005SF | 2.00 | 2.20 | 1.20 | 1.50 | 0.40 | 0.90 | 0.20 | 0.10 |
| SMD0805R010SF | 2.00 | 2.20 | 1.20 | 1.50 | 0.40 | 0.90 | 0.20 | 0.10 |
| SMD0805R020SF | 2.00 | 2.20 | 1.20 | 1.50 | 0.35 | 0.80 | 0.20 | 0.10 |
| SMD0805R035SF | 2.00 | 2.20 | 1.20 | 1.50 | 0.35 | 0.80 | 0.20 | 0.10 |
| SMD0805R035SF12v | 2.00 | 2.20 | 1.20 | 1.50 | 0.35 | 0.80 | 0.20 | 0.10 |
| SMD0805R050SF | 2.00 | 2.20 | 1.20 | 1.50 | 0.35 | 0.80 | 0.20 | 0.10 |
| SMD0805R050SF12v | 2.00 | 2.20 | 1.20 | 1.50 | 0.35 | 0.80 | 0.20 | 0.10 |
| SMD0805R050SF16v | 2.00 | 2.20 | 1.20 | 1.50 | 0.50 | 1.10 | 0.20 | 0.10 |
| SMD0805R050SF24v | 2.00 | 2.20 | 1.20 | 1.50 | 0.50 | 1.10 | 0.20 | 0.10 |
| SMD0805R075SF | 2.00 | 2.20 | 1.20 | 1.50 | 0.50 | 1.00 | 0.20 | 0.10 |
| SMD0805R075SF12v | 2.00 | 2.20 | 1.20 | 1.50 | 0.50 | 1.00 | 0.20 | 0.10 |
| SMD0805R100SF | 2.00 | 2.20 | 1.20 | 1.50 | 0.70 | 1.20 | 0.20 | 0.10 |
| SMD0805R100SF12v | 2.00 | 2.20 | 1.20 | 1.50 | 0.70 | 1.20 | 0.20 | 0.10 |
| SMD0805R110SF | 2.00 | 2.20 | 1.20 | 1.50 | 0.70 | 1.20 | 0.20 | 0.10 |
| SMD0805R110SF12v | 2.00 | 2.20 | 1.20 | 1.50 | 0.70 | 1.20 | 0.20 | 0.10 |
| SMD0805R125SF | 2.00 | 2.20 | 1.20 | 1.50 | 1.00 | 1.50 | 0.20 | 0.10 |
| SMD0805R150SF | 2.00 | 2.20 | 1.20 | 1.50 | 1.00 | 1.50 | 0.20 | 0.10 |

Termination Pad Characteristics

Terminal pad materials：Tin-plated Nickel-Copper

Terminal pad solder ability：Meets EIA specification RS186-9E and ANSI/J-STD-002 Category 3.

Recommended Pad Layout (mm.)

Packaging Quantity

| Part Number | Quantity |
| --- | --- |
| SMD0805R005.010.020.035.050.SF | 5,000 pcs/reel |
| SMD0805R075.100.110.125.SF | 4,000 pcs/reel |
| SMD0805R150SF | 3,500 pcs/reel |

Tape & reel packaging per EIA481-1

Tape And Reel Specifications (mm)

| Governing Specifications | EIA 481-1 |
| --- | --- |
| W |  | 8.0 ± 0.3 |
| P0 |  | 4.0 ± 0.10 |
| P1 |  | 4.0 ± 0.10 |
| P2 |  | 2.0 ± 0.05 |
| A0 |  | 1.45 ± 0.10 |
| B0 |  | 2.30 ± 0.10 |
| B1max. |  | 4.35 |
| D0 |  | 1.55 + 0.1, -0 |
| F |  | 3.5 ± 0.05 |
| E1 |  | 1.75 ± 0.10 |
| E2min. |  | 6.25 |
| T |  | 0.25 |
| T1max. |  | 0.1 |
| K0 |  | 0.74 ± 0.1 |
| Leader min. |  | 390 |
| Trailer min. |  | 160 |
| Reel Dimensions |  |
| A max. |  | 178 |
| N min. |  | 60 |
| W1 |  | 9.0 ± 0.5 |
| W2 |  | 12.0 ± 0.05 |
| Storage And Handling |
| ‧ Storage conditions：35°C max, 30%-60% R.H. |
| ‧ Devices may not meet specified performance |
| if storage conditions are exceeded. |

Part Number System

SMD 0805 R 口口口 S F 口口V
                                           special voltage Rating(Optional)

Lead-Free

Tin-plated Nickel-Copper

Holding Current Rating

Da Rong

Device Dimensions: Length/width(Unit:1/100 inch) Size 2012 mm / 0805 inch

Surface Mount Device

# Text boxes

t L

60~150 s

ts

Preheat 60~180 s

t 25°C to peak

Time

TL 217

TP 260

25

TP 20~40 S

Ramp-up

Critical Zone

TL to TP

Ramp-down

Tsmax

Tsmin

150

200

A

B

D

E

C

1

1.2士0.1

1.0士0.1

1.0 士0.1

1.5士0.1

P1

W

E2

F

E1

P0

P2

B0

K0

B1

T1

Cover tape

D0

A0

Embossment

T

EIA Tape Component Dimensions

Embossed cavity

Cover tape

Carrier tape

A

W2(measured at hub)

N(hub dia.)

W1(measured at hub)

2

2

2

0

EIA Reel Dimensions