APPROVAL SHEET

MODEL NO.：

CUSTOMER：

CUSTOMER'S APPROVAL： AUTHORIZED SIGNATURE/STAMP DATE

MANUFACTURER: LaoHuLing Industrial Area, XiaoJinKou Town, HuiCheng District, HuiZhou City, GuangDong Province, CHINA Tel: 0752-7213069/7213070 Fax: 0752-7213065 Submitted by: Approved by: Date:

Performance Specification

| Model | Marking |  |  |  |  |  | Maximum | Resistance | 认证 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | V max | Imax | I hold | I trip | Pd | Time To Trip |  |  |
|  |  |  |  | @25°C | @25°C | Typ. | Current | Time | R i min | R1max | UL |
|  |  | (V dc) | (A) | (A) | (A) | (W) | (A) | (Sec) | () | () |  |
| SMD0603R001SF | X | 60 | 20 | 0.01 | 0.03 | 0.5 | 0.2 | 1.00 | 15.000 | 100.000 |  |
| SMD0603R002SF | Y | 60 | 20 | 0.02 | 0.06 | 0.5 | 0.2 | 1.00 | 12.000 | 70.000 |  |
| SMD0603R002SF9v | Y | 9 | 20 | 0.02 | 0.06 | 0.5 | 0.2 | 1.00 | 12.000 | 70.000 | √ |
| SMD0603R003SF | Z | 30 | 20 | 0.03 | 0.09 | 0.5 | 0.2 | 1.00 | 6.000 | 50.000 |  |
| SMD0603R003SF9v | Z | 9 | 20 | 0.03 | 0.09 | 0.5 | 0.2 | 1.00 | 6.000 | 50.000 | √ |
| SMD0603R004SF | - | 24.0 | 20 | 0.04 | 0.12 | 0.5 | 0.20 | 1.00 | 4.000 | 40.000 |  |
| SMD0603R005SF | - | 15.0 | 20 | 0.05 | 0.15 | 0.5 | 0.25 | 1.00 | 3.800 | 30.000 |  |
| SMD0603R005SF9v | - | 9.0 | 20 | 0.05 | 0.15 | 0.5 | 0.25 | 1.00 | 3.800 | 30.000 | √ |
| SMD0603R010SF | 1 | 15.0 | 35 | 0.10 | 0.30 | 0.5 | 0.5 | 1.00 | 0.900 | 6.000 |  |
| SMD0603R010SF9v | 1 | 9.0 | 35 | 0.10 | 0.30 | 0.5 | 0.5 | 1.00 | 0.900 | 6.000 | √ |
| SMD0603R020SF | 2 | 9.0 | 35 | 0.20 | 0.50 | 0.5 | 1.0 | 0.60 | 0.550 | 3.500 | √ |
| SMD0603R020SF16v | 2 | 16.0 | 35 | 0.20 | 0.50 | 0.5 | 1.0 | 0.60 | 0.550 | 3.500 |  |
| SMD0603R025SF | 2 | 9.0 | 35 | 0.25 | 0.55 | 0.5 | 8.0 | 0.08 | 0.500 | 3.000 | √ |
| SMD0603R025SF16v | 2 | 16.0 | 35 | 0.25 | 0.55 | 0.5 | 8.0 | 0.08 | 0.500 | 3.000 |  |
| SMD0603R035SF | 3 | 6.0 | 35 | 0.35 | 0.75 | 0.5 | 8.0 | 0.10 | 0.200 | 1.000 |  |
| SMD0603R040SF | 5 | 6.0 | 35 | 0.40 | 0.80 | 0.5 | 8.0 | 0.10 | 0.150 | 0.900 |  |
| SMD0603R050SF | 5 | 6.0 | 35 | 0.50 | 1.00 | 0.5 | 8.0 | 0.10 | 0.100 | 0.800 |  |
| SMD0603R050SF12v | 5 | 12.0 | 35 | 0.50 | 1.00 | 0.5 | 8.0 | 0.10 | 0.100 | 0.800 |  |
| SMD0603R060SF | 7 | 6.0 | 35 | 0.60 | 1.20 | 0.5 | 8.0 | 0.10 | 0.080 | 0.600 |  |
| SMD0603R065SF | 7 | 6.0 | 35 | 0.65 | 1.30 | 0.5 | 8.0 | 0.10 | 0.070 | 0.550 |  |
| SMD0603R075SF | 7 | 6.0 | 35 | 0.75 | 1.40 | 0.5 | 8.0 | 0.10 | 0.060 | 0.450 |  |
| SMD0603R100SF | 0 | 6.0 | 35 | 1.00 | 2.00 | 0.5 | 8.0 | 0.10 | 0.050 | 0.300 |  |

V max  = Maximum operating voltage device can withstand without damage at rated current (Imax).

I max   = Maximum fault current device can withstand without damage at rated voltage (V max).

I hold   = Hold Current. Maximum current device will not trip in 25°C still air.

I trip    = Trip Current. Minimum current at which the device will always trip in 25°C still air.

Pd      = Power dissipation when device is in the tripped state in 25°C still air environment at rated voltage.

Ri min/max  = Minimum/Maximum device resistance prior to tripping at 25°C.

R1max  = Maximum device resistance is measured one hour post reflow.

CAUTION : Operation beyond the specified ratings may result in damage and possible arcing and flame.

Environmental Specifications

| Test |  |  |  | Conditions |  |  |  | Resistance change |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Passive aging |  |  |  | +85°C, 1000 hrs. |  |  | ±5% typical |  |  |
| Humidity aging |  |  |  | +85°C, 85% R.H. , 168 hours |  | ±5% typical |  |  |
| Thermal shock |  |  |  | +85°C to -40°C, 20 times |  |  | ±33% typical |  |
| Resistance to solvent |  |  |  | MIL-STD-202,Method 215 |  |  | No change |  |  |
| Vibration |  |  |  | MIL-STD-202,Method 201 |  |  | No change |  |  |
| Ambient operating conditions : - 40 °C to +85 °C |
| Maximum surface temperature of the device in the tripped state is 125 °C |

Agency Approval and Environmental Complianc

| Agency | File Number |  | Regulation | Standard |
| --- | --- | --- | --- | --- |
| UL | E486890 |  |  | 2011/65/EU |
| TUV | pending |  |  | EN14582 |

Thermal Derading Chart

Recommended Hold Current(A) at Ambient Temperature(°C)

| Model | Ambient Operation Temperature |
| --- | --- |
|  | -40°C | -20°C | 0°C | 25°C | 40°C | 50°C | 60°C | 70°C | 85°C |
| SMD0603R001SF | 0.016 | 0.014 | 0.012 | 0.010 | 0.008 | 0.007 | 0.006 | 0.005 | 0.0035 |
| SMD0603R002SF | 0.031 | 0.027 | 0.024 | 0.020 | 0.016 | 0.014 | 0.012 | 0.011 | 0.007 |
| SMD0603R003SF | 0.047 | 0.041 | 0.036 | 0.030 | 0.024 | 0.021 | 0.018 | 0.016 | 0.0108 |
| SMD0603R004SF | 0.052 | 0.048 | 0.044 | 0.040 | 0.032 | 0.028 | 0.024 | 0.020 | 0.012 |
| SMD0603R005SF | 0.065 | 0.060 | 0.055 | 0.050 | 0.040 | 0.035 | 0.031 | 0.025 | 0.015 |
| SMD0603R010SF | 0.13 | 0.12 | 0.11 | 0.10 | 0.08 | 0.07 | 0.06 | 0.05 | 0.03 |
| SMD0603R020SF | 0.27 | 0.25 | 0.23 | 0.20 | 0.17 | 0.14 | 0.12 | 0.10 | 0.07 |
| SMD0603R025SF | 0.32 | 0.29 | 0.27 | 0.25 | 0.21 | 0.18 | 0.16 | 0.14 | 0.10 |
| SMD0603R035SF | 0.47 | 0.41 | 0.38 | 0.35 | 0.29 | 0.26 | 0.24 | 0.20 | 0.14 |
| SMD0603R040SF | 0.54 | 0.47 | 0.43 | 0.40 | 0.33 | 0.29 | 0.27 | 0.22 | 0.16 |
| SMD0603R050SF | 0.67 | 0.59 | 0.54 | 0.50 | 0.41 | 0.37 | 0.34 | 0.29 | 0.20 |
| SMD0603R060SF | 0.81 | 0.70 | 0.651 | 0.60 | 0.49 | 0.44 | 0.41 | 0.34 | 0.24 |
| SMD0603R065SF | 0.87 | 0.76 | 0.71 | 0.65 | 0.54 | 0.48 | 0.44 | 0.37 | 0.26 |
| SMD0603R075SF | 0.98 | 0.85 | 0.81 | 0.75 | 0.60 | 0.54 | 0.44 | 0.40 | 0.31 |
| SMD0603R100SF | 1.19 | 1.13 | 1.08 | 1.00 | 0.80 | 0.72 | 0.59 | 0.54 | 0.43 |

Thermal Derating Curve                Average Time-Current Curve

Soldering Parameters

| Profile Feature | Pb-Free Assembly |
| --- | --- |
| Average Ramp-Up Rate(Ts max to T p) | 3℃/second mac. |
| Preheat -Temperature Min(Ts min) -Temperature Max(Ts max) -Time(Ts min to Ts max) | 150℃ 200℃ 60~180 seconds |
| Time maintained above: -Temperature(TL) -Time(tL) | 217℃ 60~150 seconds |
| Peak Temperature(Tp) | 260℃ |
| Ramp-Down Rate | 6℃/second max. |
| Time 25℃ to Peak Temperature | 8 minutes max |
| Storage Condition | 0℃~35℃,30%-60%RH |

Recommended reflow methods: IR, vapor phase oven, hot air oven, N2 environment for lead-free

Recommended maximum paste thickness is 0.25mm

Devices can be cleaned using standard industry methods and solvents.

Note 1:All temperature refer to topside of the package, measured on the package body surface.

Note 2: If reflow temperatures exceed the recommended profile, devices may not meet the performance requirements

Physical Dimensions(mm.)

| 型號 | A | B | C | D | E |
| --- | --- | --- | --- | --- | --- |
|  | Min. | Max. | Min. | Max. | Min. | Max. | Min. | Min. |
| SMD0603R001SF | 1.45 | 1.85 | 0.65 | 1.05 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD0603R002SF9v | 1.45 | 1.85 | 0.65 | 1.05 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD0603R002SF | 1.45 | 1.85 | 0.65 | 1.05 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD0603R003SF9v | 1.45 | 1.85 | 0.65 | 1.05 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD0603R003SF | 1.45 | 1.85 | 0.65 | 1.05 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD0603R004SF | 1.45 | 1.85 | 0.65 | 1.05 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD0603R005SF9v | 1.45 | 1.85 | 0.65 | 1.05 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD0603R005SF | 1.45 | 1.85 | 0.65 | 1.05 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD0603R010SF9v | 1.45 | 1.85 | 0.65 | 1.05 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD0603R010SF | 1.45 | 1.85 | 0.65 | 1.05 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD0603R020SF | 1.45 | 1.85 | 0.65 | 1.05 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD0603R020SF16v | 1.45 | 1.85 | 0.65 | 1.05 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD0603R025SF | 1.45 | 1.85 | 0.65 | 1.05 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD0603R025SF16v | 1.45 | 1.85 | 0.65 | 1.05 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD0603R035SF | 1.45 | 1.85 | 0.65 | 1.05 | 0.35 | 0.90 | 0.15 | 0.10 |
| SMD0603R040SF | 1.45 | 1.85 | 0.65 | 1.05 | 0.40 | 0.90 | 0.15 | 0.10 |
| SMD0603R050SF | 1.45 | 1.85 | 0.65 | 1.05 | 0.55 | 1.15 | 0.15 | 0.10 |
| SMD0603R050SF12v | 1.45 | 1.85 | 0.65 | 1.05 | 0.55 | 1.15 | 0.15 | 0.10 |
| SMD0603R060SF | 1.45 | 1.85 | 0.65 | 1.05 | 0.55 | 1.15 | 0.15 | 0.10 |
| SMD0603R065SF | 1.45 | 1.85 | 0.65 | 1.05 | 0.55 | 1.15 | 0.15 | 0.10 |
| SMD0603R075SF | 1.45 | 1.85 | 0.65 | 1.05 | 0.55 | 1.15 | 0.15 | 0.10 |
| SMD0603R100SF | 1.45 | 1.85 | 0.65 | 1.05 | 0.55 | 1.15 | 0.15 | 0.10 |

Termination Pad Characteristics

Terminal pad materials：Tin-plated Nickel-Copper

Terminal pad solder ability：Meets EIA specification RS186-9E and ANSI/J-STD-002 Category 3.

Recommended Pad Layout (mm.)

Packaging Quantity

| Part Number | Quantity |
| --- | --- |
| SMD0603 HF Series | 4,000 pcs/reel |

Tape & reel packaging per EIA481-1

Tape And Reel Specifications (mm)

| Governing Specifications | EIA 481-1 |
| --- | --- |
| W |  | 8.0 ± 0.2 |
| P0 |  | 4.0 ± 0.10 |
| P1 |  | 4.0 ± 0.10 |
| P2 |  | 2.0 ± 0.05 |
| A0 |  | 1.05 ± 0.10 |
| B0 |  | 1.85 ± 0.10 |
| D0 |  | 1.55 + 0.05 |
| F |  | 3.5 ± 0.05 |
| E1 |  | 1.75 ± 0.10 |
| E2min. |  | 6.25 |
| T |  | 0.20 |
| T1max. |  | 0.1 |
| K0 |  | 0.75/0.95 ± 0.1 |
| Leader min. |  | 390 |
| Trailer min. |  | 160 |
| 卷軸規格 |  |
| A max. |  | 178 |
| N min. |  | 60 |
| W1 |  | 9.0 ± 0.5 |
| W2 |  | 12.0 ± 0.05 |
| W |  | 8.0 ± 0.2 |
| Storage And Handling |
| ‧ Storage conditions：35°C max, 30%-60% R.H. |
| ‧ Devices may not meet specified performance |
| if storage conditions are exceeded. |

Part Number System

SMD 0603 R 口口口 S F 口口V
                                           special voltage Rating(Optional)

Lead-Free

Tin-plated Nickel-Copper

Holding Current Rating

Da Rong

Device Dimensions: Length/width(Unit:1/100 inch) Size1608mm / 0603 inch

Surface Mount Device

# Text boxes

t L

60~150 s

ts

Preheat 60~180 s

t 25°C to peak

Time

TL 217

TP 260

25

TP 20~40 S

Ramp-up

Critical Zone

TL to TP

Ramp-down

Tsmax

Tsmin

150

200

A

B

D

E

C

3

1.0士0.1

1.0士0.1

1.0 士0.1

1.0士0.1

P1

W

E2

F

E1

P0

P2

B0

K0

B1

T1

Cover tape

D0

A0

Embossment

T

EIA Tape Component Dimensions

Embossed cavity

Cover tape

Carrier tape

A

W2(measured at hub)

N(hub dia.)

W1(measured at hub)

2

2

2

0

EIA Reel Dimensions