APPROVAL SHEET

MODEL NO.：                                              SMD0805 HF Series

CUSTOMER：

CUSTOMER'S APPROVAL： AUTHORIZED SIGNATURE/STAMP DATE

MANUFACTURER: The Fourth Industrial Zone,Luokeng Village, Xiaotie District, Xiaojinkou Town, Huizhou City, Guangdong Province, China Tel: 0752-7213069/7213070 Fax: 0752-7213065 Submitted by: Approved by: Date:

Performance Specification

|  |  |  | Vmax |  |  | Maximum Time | Resistance |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Ihold | Itrip |  | Imax | Pd | To Trip |  |
|  | (A) | (A) | (Vdc) | (A) | Typ. | Current | Time | Rimin. | Rimax. | R1max |
|  |  |  |  |  | (W) | (A) | (Sec) | (Ω) | (Ω) | (Ω) |
| 135R050 | 0.05 | 0.10 | 135 | 2.5 | 0.27 | 0.25 | 4.0 | 12.0 | 27.0 | 36.0 |
| 135R060 | 0.06 | 0.12 | 135 | 3.0 | 0.30 | 0.30 | 4.0 | 10.0 | 22.0 | 30 |
| 135R080 | 0.08 | 0.16 | 135 | 4.0 | 0.38 | 0.40 | 4.0 | 6.0 | 13.0 | 18.0 |
| 135R100 | 0.10 | 0.20 | 135 | 5.0 | 0.40 | 0.50 | 5.0 | 4.5 | 10.0 | 13.5 |
| 135R120 | 0.12 | 0.24 | 135 | 6.0 | 0.46 | 0.60 | 6.0 | 3.5 | 8.0 | 10.5 |
| 135R160 | 0.16 | 0.32 | 135 | 6.0 | 0.50 | 0.80 | 7.0 | 2.0 | 4.5 | 6.0 |
| 135R200 | 0.20 | 0.40 | 135 | 6.0 | 0.72 | 1.00 | 5.0 | 2.0 | 4.5 | 6.0 |
| 135R250 | 0.25 | 0.50 | 135 | 6.0 | 0.9 | 1.25 | 5.0 | 1.6 | 3.6 | 4.8 |
| 135R300 | 0.30 | 0.60 | 135 | 6.0 | 1.0 | 1.50 | 5.0 | 1.35 | 3.0 | 3.6 |
| 135R400 | 0.40 | 0.80 | 135 | 6.0 | 1.3 | 2.0 | 5.0 | 0.90 | 2.0 | 2.4 |
| 135R500 | 0.50 | 1.0 | 135 | 7.5 | 1.6 | 2.50 | 5.0 | 0.70 | 1.55 | 1.9 |
| 135R550 | 0.55 | 1.1 | 135 | 7.5 | 1.6 | 2.75 | 5.0 | 0.60 | 1.45 | 1.75 |
| 135R650 | 0.65 | 1.3 | 135 | 7.5 | 1.7 | 3.25 | 8.0 | 0.50 | 1.10 | 1.35 |
| 135R750 | 0.75 | 1.5 | 135 | 7.5 | 1.8 | 3.75 | 8.0 | 0.35 | 0.80 | 0.96 |
| 135R900 | 0.90 | 1.8 | 135 | 9.0 | 2.1 | 4.5 | 8.0 | 0.27 | 0.60 | 0.72 |
| 135R1000 | 1.00 | 2.0 | 135 | 10.0 | 2.2 | 5.0 | 8.0 | 0.25 | 0.55 | 0.66 |
| 135R1100 | 1.10 | 2.2 | 135 | 11.0 | 2.4 | 5.50 | 9.0 | 0.22 | 0.50 | 0.6 |
| 135R1250 | 1.25 | 2.5 | 135 | 12.5 | 2.6 | 6.25 | 10.0 | 0.18 | 0.4 | 0.48 |
| 135R1350 | 1.35 | 2.7 | 135 | 13.5 | 2.8 | 6.75 | 10.0 | 0.16 | 0.36 | 0.43 |
| 135R1600 | 1.60 | 3.2 | 135 | 16.0 | 3.2 | 8.0 | 10.0 | 0.13 | 0.27 | 0.33 |
| 135R1850 | 1.85 | 3.7 | 135 | 18.5 | 3.6 | 9.25 | 10.0 | 0.11 | 0.22 | 0.27 |
| 135R2000 | 2.00 | 4.0 | 135 | 20.0 | 3.9 | 10.0 | 12.0 | 0.10 | 0.20 | 0.24 |
| 135R2500 | 2.50 | 5.0 | 135 | 20.0 | 4.6 | 12.5 | 15.0 | 0.075 | 0.15 | 0.18 |
| 135R3000 | 3.00 | 6.0 | 135 | 20.0 | 5.3 | 15.0 | 15.0 | 0.06 | 0.12 | 0.15 |
| 135R3500 | 3.50 | 7.0 | 135 | 20.0 | 6.0 | 17.5 | 15.0 | 0.050 | 0.10 | 0.12 |

V max  = Maximum operating voltage device can withstand without damage at rated current (Imax).

I max   = Maximum fault current device can withstand without damage at rated voltage (V max).

I hold   = Hold Current. Maximum current device will not trip in 25°C still air.

I trip    = Trip Current. Minimum current at which the device will always trip in 25°C still air.

Pd      = Power dissipation when device is in the tripped state in 25°C still air environment at rated voltage.

Ri min/max  = Minimum/Maximum device resistance prior to tripping at 25°C.

R1max  = Maximum device resistance is measured one hour post reflow.

CAUTION : Operation beyond the specified ratings may result in damage and possible arcing and flame.

Environmental Specifications

| Test |  |  |  | Conditions |  |  |  | Resistance change |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Passive aging |  |  |  | +85°C, 1000 hrs. |  |  | ±5% typical |  |  |
| Humidity aging |  |  |  | +85°C, 85% R.H. , 168 hours |  | ±5% typical |  |  |
| Thermal shock |  |  |  | +85°C to -40°C, 20 times |  |  | ±33% typical |  |
| Resistance to solvent |  |  |  | MIL-STD-202,Method 215 |  |  | No change |  |  |
| Vibration |  |  |  | MIL-STD-202,Method 201 |  |  | No change |  |  |
| Ambient operating conditions : - 40 °C to +85 °C |
| Maximum surface temperature of the device in the tripped state is 125 °C |

Agency Approval and Environmental Complianc

| Agency | File Number |  | Regulation | Standard |
| --- | --- | --- | --- | --- |
| UL | pending |  |  | 2002/95/EC |
| TUV | pending |  |  | EN14582 |

Thermal Derating Curve

Average Time-Current Curve

| A=135R050 | J=135R400 | S=135R1350 |
| --- | --- | --- |
| B=135R060 | K=135R500 | T=135R1600 |
| C=135R080 | L=135R550 | U=135R1850 |
| D=135R100 | M=135650 | V=135R2500 |
| E=135R120 | N=135R750 | W=135R2500 |
| F=135R160 | O=135900 | X=135R3000 |
| G=135R200 | P=135R1000 | Y=135R3500 |
| H=135R250 | Q=135R1100 |  |
| I=135R300 | R=135R1250 |  |

Ihold Versus Temperature

| 型號 | 最高環境溫度和保持電流 |
| --- | --- |
|  | -40°C | -20°C | 0°C | 25°C | 40°C | 50°C | 60°C | 70°C | 85°C |
| 135R050 | 0.078 | 0.068 | 0.060 | 0.05 | 0.041 | 0.036 | 0.032 | 0.027 | 0.020 |
| 135R060 | 0.093 | 0.082 | 0.071 | 0.06 | 0.049 | 0.043 | 0.038 | 0.032 | 0.024 |
| 135R080 | 0.124 | 0.109 | 0.095 | 0.08 | 0.065 | 0.058 | 0.050 | 0.043 | 0.032 |
| 135R100 | 0.155 | 0.136 | 0.119 | 0.10 | 0.081 | 0.072 | 0.063 | 0.054 | 0.040 |
| 135R120 | 0.486 | 0.163 | 0.143 | 0.12 | 0.097 | 0.086 | 0.076 | 0.065 | 0.048 |
| 135R160 | 0.248 | 0.218 | 0.190 | 0.16 | 0.130 | 0.115 | 0.101 | 0.086 | 0.064 |
| 135R200 | 0.31 | 0.27 | 0.24 | 0.20 | 0.16 | 0.14 | 0.13 | 0.11 | 0.08 |
| 135R250 | 0.39 | 0.34 | 0.30 | 0.25 | 0.20 | 0.18 | 0.16 | 0.14 | 0.10 |
| 135R300 | 0.47 | 0.41 | 0.36 | 0.30 | 0.24 | 0.22 | 0.20 | 0.16 | 0.12 |
| 135R400 | 0.62 | 0.54 | 0.48 | 0.40 | 0.32 | 0.29 | 0.25 | 0.22 | 0.16 |
| 135R500 | 0.78 | 0.68 | 0.60 | 0.50 | 0.41 | 0.36 | 0.32 | 0.27 | 0.20 |
| 135R550 | 0.85 | 0.75 | 0.66 | 0.55 | 0.45 | 0.40 | 0.35 | 0.30 | 0.22 |
| 135R650 | 1.01 | 0.88 | 0.77 | 0.65 | 0.53 | 0.47 | 0.41 | 0.35 | 0.26 |
| 135R750 | 1.16 | 1.02 | 0.89 | 0.75 | 0.61 | 0.54 | 0.47 | 0.41 | 0.30 |
| 135R900 | 1.4 | 1.22 | 1.07 | 0.90 | 0.73 | 0.65 | 0.57 | 0.49 | 0.36 |
| 135R1000 | 1.55 | 1.36 | 1.19 | 1.00 | 0.81 | 0.72 | 0.63 | 0.54 | 0.40 |
| 135R1100 | 1.71 | 1.5 | 1.31 | 1.1 | 0.89 | 0.79 | 0.69 | 0.59 | 0.44 |
| 135R1250 | 1.94 | 1.7 | 1.49 | 1.25 | 1.01 | 0.9 | 0.79 | 0.68 | .0.50 |
| 135R1350 | 2.09 | 1.84 | 1.61 | 1.35 | 1.09 | 0.97 | 0.85 | 0.73 | 0.54 |
| 135R1600 | 2.48 | 2.18 | 1.9 | 1.6 | 1.30 | 1.15 | 1.01 | 0.86 | 0.64 |
| 135R1850 | 2.87 | 2.52 | 2.20 | 1.85 | 1.50 | 1.33 | 1.17 | 1.00 | 0.74 |
| 135R2000 | 3.10 | 2.72 | 2.38 | 2.00 | 1.62 | 1.44 | 1.26 | 1.08 | 0.80 |
| 135R2500 | 3.88 | 3.40 | 2.98 | 2.50 | 2.03 | 1.80 | 1.58 | 1.35 | 1.00 |
| 135R3000 | 4.65 | 4.08 | 3.57 | 3.00 | 2.43 | 2.16 | 1.89 | 1.62 | 1.20 |
| 135R3500 | 5.43 | 4.76 | 4.17 | 3.50 | 2.84 | 2.52 | 2.21 | 1.89 | 1.40 |

Soldering Parameters

| WAVE SOLDERING INFORMATIONS |
| --- |
| Pre-Heating Zone | Max. ramping rate should not exceed 4℃/Sec. |
| Soldering Zone | Max. solder temperature should not exceed 260℃ |
| Cooling Zone | Cooling by natural convection in air. |
| ◎Specifications are subject to change without notice. |

Physical Dimensions(mm.)

1型               2型

| 型號 | A | B | C | D | E | Lead |
| --- | --- | --- | --- | --- | --- | --- |
|  | Max. | Max. | Max. | Min. | Typ. | Style | 直径（Φ） |
| 135R050 | 6.0 | 8.3 | 3.8 | 7.6 | 5.1 | 1 | 0.5 |
| 135R060 | 6.0 | 8.7 | 3.8 | 7.6 | 5.1 | 1 | 0.5 |
| 135R080 | 6.0 | 9.3 | 3.8 | 7.6 | 5.1 | 1 | 0.5 |
| 135R100 | 6.0 | 10.0 | 3.8 | 7.6 | 5.1 | 1 | 0.5 |
| 135R120 | 7.0 | 10.5 | 3.8 | 7.6 | 5.1 | 1 | 0.5 |
| 135R160 | 7.0 | 10.5 | 3.8 | 7.6 | 5.1 | 2 | 0.5 |
| 135R200 | 6.5 | 10.0 | 3.8 | 7.6 | 5.1 | 2 | 0.5 |
| 135R250 | 7.0 | 10.5 | 3.8 | 7.6 | 5.1 | 2 | 0.6 |
| 135R300 | 6.5 | 13.0 | 3.8 | 7.6 | 5.1 | 2 | 0.6 |
| 135R400 | 8.8 | 14.5 | 3.8 | 7.6 | 5.1 | 2 | 0.6 |
| 135R500 | 8.8 | 14.5 | 3.8 | 7.6 | 5.1 | 2 | 0.8 |
| 135R550 | 8.8 | 14.5 | 3.8 | 7.6 | 5.1 | 2 | 0.8 |
| 135R650 | 10.0 | 15.0 | 3.8 | 7.6 | 5.1 | 2 | 0.8 |
| 135R750 | 10.0 | 16.5 | 3.8 | 7.6 | 5.1 | 2 | 0.8 |
| 135R900 | 11.3 | 17.5 | 3.8 | 7.6 | 5.1 | 2 | 0.8 |
| 135R1000 | 12.0 | 21.0 | 3.8 | 7.6 | 5.1 | 2 | 0.8 |
| 135R1100 | 13.5 | 18.8 | 3.8 | 7.6 | 5.1 | 2 | 0.8 |
| 135R1250 | 14.0 | 22.2 | 3.8 | 7.6 | 5.1 | 2 | 0.8 |
| 135R1350 | 15.7 | 23.7 | 3.8 | 7.6 | 5.1 | 2 | 0.8 |
| 135R1600 | 15.7 | 23.7 | 3.8 | 7.6 | 5.1 | 2 | 0.8 |
| 135R1850 | 16.0 | 24.5 | 3.8 | 7.6 | 10.2 | 2 | 0.8 |
| 135R2000 | 18.5 | 25.5 | 3.8 | 7.6 | 10.2 | 2 | 0.8 |
| 135R2500 | 21.0 | 29.0 | 3.8 | 7.6 | 10.2 | 2 | 0.8 |
| 135R3000 | 24.5 | 29.0 | 3.8 | 7.6 | 10.2 | 2 | 0.8 |
| 135R3500 | 24.5 | 33.5 | 3.8 | 7.6 | 10.2 | 2 | 0.8 |

PHYSICAL SPECIFICATIONS :

Materials : Leads 135R050 ~ 200: Tin-platedcopper-cladsteel,0.205mm2(24AWG),Φ0.50mm(0.020in).

135R250 ~ 400: Tin-plated copper, 0.52mm2  (20AWG), Φ0.60mm(0.032 in).

135R500 ~ 3500: Tin-plated copper, 0.52mm2  (20AWG), Φ0.80mm(0.032 in).

Lead Solderability : MIL-STD-202, Method 208E

Packaging Quantity

| 135 | 3500 | U | Model | Reel Q'ty | Bag Q'ty |
| --- | --- | --- | --- | --- | --- |
| Radial type | Hold | U= Bulk | 135R050-135R750 | - | 1000 |
| 135V | Current(A):3.50A | packaged | 135R900-135R1600 | - | 500 |
|  |  |  | 135R1850135R2500 |  | 200 |
|  |  |  | 135R3000-135R3500 |  | 100 |

Tape & Reel packaging per EIA468-B standard.

# Text boxes

Time

TP 260

100

25

Soldering

5Sea.MAX

Gradual

Cooling

Pre-Heating

1 Minute Min.

R =商標

135= 135 Vrms 工作電壓

080= 0.08A 保持電流

XXX=日期

Y=代碼

R135

080

XXXY